## Slide 1
April 2012
Improving Remediation Planning through Effective Mine Material Delineation
Formosa Mine Superfund Site, Douglas County, OR
Mark Nelson PG
Nicholas Anton PE
Howard Young LG

## Slide 2: Why would one delineate mine materials?
Understand potential connections between suspect source materials and observed water quality effects
Delineate problematic materials
Support remedial action decisions
Active Mine Projects
Manage potential environmental liabilities
Comply with environmental regulations
Cause?
Effects?
Mine Remediation Projects

## Slide 3: What are mine materials?
Tailings
Spent ore
Waste rock
Highwalls
Mine Materials are potential source materials for dissolved metals in surface water and groundwater

## Slide 4: Effective Mine Material Delineation
Mine Remediation Projects
Supports
  Accurate alternative assessment
  Reasonable cost estimates
  Sound remedial action decisions
  Effective remedial designs
  Successful remediation
Data often support multi-million dollar decisions
Active Mining Projects
Supports
  Mine permitting activities
  Environmental management
  Successful reclamation
Manages potential environmental liabilities
  Clean Water Act, CERCLA
  Various state environmental laws
Improving Remediation Planning though Effective Mine Material Delineation, Formosa Mine Superfund Site

## Slide 5: Approach to Data Collection and Analysis
Rapid field geochemical characterization
  Triad approach
    Save costs throughout project lifecycle
    Utilize field tools for real time measurements
    Conduct laboratory verification
  Components
    Lithological examination, field paste pH, FPXRF
    Real time geospatial database
    Coupled laboratory analysis
      Acid base accounting
      Extraction tests
      Total metals analysis
Weight of evidence statistical approach
Improving Remediation Planning though Effective Mine Material Delineation, Formosa Mine Superfund Site

## Slide 6: Approach can be applied at various project phases and in various levels of detail
Reconnaissance Phase
  Quick field survey
  Limited or no laboratory verification
  Qualitative data analysis
Site Characterization Phase
  More detailed surveys
  Laboratory verification
  Statistical data analyses
Reclamation or remediation phase
  Confirmatory sampling
  Detailed surveys
  Lab verification
  Statistical data analysis
Formosa is a good example of a comprehensive site characterization phase program
Formosa Mine- West Encapsulation Mound Waste Rock Dump

## Slide 7: Interdisciplinary Field Team
  Geologist
    Identifies mineralized rock based on lithology, alteration, and mineralization
    Guides dynamic work strategies based on geology and other visual indicators of mine materials
  Environmental scientist
    Collects field paste pH and FPXRF measurements
    Collects samples for laboratory analysis
  Field technician
    Collects GPS data using a resource grade instrument (<1m accuracy)
Improving Remediation Planning though Effective Mine Material Delineation, Formosa Mine Superfund Site

## Slide 8: Coupled Laboratory Analyses
Acid base accounting
  Modified Sobek (1978) method
  Estimates propensity of sample to generate ARD in the future
Extraction Tests
  Modified Synthetic Precipitation Leach Procedure
  Estimates propensity of sample to leach metals and metalloids when exposed to percolating water
Total Metals Analyses
  Provides information regarding “total” content of selected metals and metalloids
SEM-EDS mineralogical analysis
  Provides information on mineralogy of samples to support ABA data interpretation
Improving Remediation Planning though Effective Mine Material Delineation, Formosa Mine Superfund Site

## Slide 9: Putting it All Together
Goals
  Identify mine materials that are causing water quality problems
  Delineate the areal extent, depth and volume of these materials
Weight of Evidence Approach
  No one laboratory analysis can answer the study questions
  Sound answers are developed with weight of evidence approach
  Components
    ARD potential
    ML potential
    Metals concentrations
Improving Remediation Planning though Effective Mine Material Delineation, Formosa Mine Superfund Site

## Slide 10: Field Paste pH Data
Improving Remediation Planning though Effective Mine Material Delineation, Formosa Mine Superfund Site
Chart: pH (su)
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8
Frequency | 10 | 91 | 99 | 58 | 54 | 7 | 4
Chart: pH (su)
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10
Frequency | 9 | 48 | 121 | 95 | 36 | 12 | 1 | 0 | 1
Surface
Subsurface
pH measured in a paste of fine grained sample and DI water
Measures products of previous sulfide oxidation and acid generation
Only appropriate for weathered mine materials
Data show Formosa mine materials to be moderately to strongly ARD generating

## Slide 11: Laboratory Acid Base Accounting Data
Improving Remediation Planning though Effective Mine Material Delineation, Formosa Mine Superfund Site
Exhibit 3.3-1. SEM-EDS photomicrograph of barite mineral grain (1), associated with chalcopyrite (2 and 3), pyrite (4), and tennantite (5).
2
4
3
5
1
Mineralogical data used to improve ABA interpretation

## Slide 12: Comparison of Field Paste Ph with ABA
Improving Remediation Planning though Effective Mine Material Delineation, Formosa Mine Superfund Site
Chart: Net Neutralization Potential (T/KT CaCO3 eq.)
| -192.72803750000003 | 3.8098249999999996 | -1.746984375 | -0.36069062500000004 | -60.839931250000006 | 0.6875 | -36.886056249999996 | -22.634243750000003 | -98.370294062500008 | -7.65959375 | -1231.244175 | -12.561431250000002 | -7.9882468750000015 | -26.440546874999988 | -5.5590093749999996 | 5.9085968750000006 | -0.92161562500000005 | -133.924884375 | -76.018946874999969 | -1481.2462137500002 | -12.185450000000003 | -53.740668750000005 | -18.93958125 | -0.31250000000000006 | -5.6037387499999989 | -0.20182499999999998 | -14.1653 | -3.3265000000000007 | -8.9732093750000015 | -3.125 | -3.125 | -22.730625 | -14.61171875 | -5.1948124999999976 | -21.677249999999994 | -3.125 | -12.516500000000002 | -6.5006875000000006 | -10.620843749999999 | -0.62500000000000011 | -30.506718750000001 | -3.2312499999999993 | -2.4399687499999998 | 22.875 | -1.8388625000000001 | -8.6147031249999984 | -6.1826875000000001 | -32.062396875000012 | -18.27380625 | -6.0855781249999996 | -14.060125000000001 | -25.158406249999995 | -60.720906250000013 | -71.757937499999983 | -27.374437500000003 | -60.992218750000013 | 8.8069687499999993 | -465.53325624999991 | -36.617781249999993 | -51.1535625 | -3.125 | 0.27074375000000001 | -11.416875000000001 | -113.37772093749999 | -2.125 | -0.48301562500000012 | -0.32938125000000007 | -6.3200343749999979 | -2.1056249999999999 | -27.413874999999997 | -0.125 | -8.3450281249999989 | -18.076484375 | 6.1310312499999986 | 4.8425906249999988 | -1.4839968749999997 | 1.6875 | 5.875 | -20.158406249999995 | -449.69211406249991 | -242.98726562500002 | -41.408271875000004 | 14.875000000000002 | -4.98095 | 13.569125 | -174.00428124999999 | -8.2919062500000003 | -70.762781249999989 | -11.523718749999999 | -4.6185968749999997 | -29.910843749999994 | -61.312887499999988 | -153.29405937500002 | -1.9751562499999999 | -4.5910625000000005 | -19.059531250000003 | -7.9775937499999996 | -3.7476250000000002 | -1.875 | -2.7373125000000007 | -7.3004374999999984 | -6.0222312499999973 | -13.216687500000001 | -7.9703125000000004 | -5.8477499999999996 | -6.9206500000000002 | -13.528593750000001
Surface Samples | 1.96 | 5.64 | 3.48 | 4.71 | 2.55 | 5.75 | 2.4 | 3.69 | 2.13 | 2.97 | 1.81 | 3.12 | 3.5 | 3.72 | 3.5 | 4.04 | 3.9 | 2.32 | 4.3 | 2.67 | 2.47 | 3.28 | 3.93 | 2.99 | 2.6 | 2.66 | 2.96 | 3.38 | 4.23 | 5.52 | 5.46 | 3.13 | 3.47 | 4 | 3.62 | 4.8 | 3.9 | 3.8 | 3.4 | 4.2 | 2.8 | 4.6 | 4.11 | 5.52 | 3.9 | 4.42 | 3.56 | 2.34 | 4 | 3.8 | 2.7 | 2.43 | 2.4 | 2.3 | 2.62 | 2.5 | 4.14 | 2.1 | 3.57 | 2.58
Subsurface Samples | 3.96 | 5.66 | 3.52 | 2.78 | 4.55 | 4.29 | 3.75 | 3.4 | 5.4 | 3.3 | 3.9 | 2.7 | 3.1 | 3.69 | 5.34 | 4.19 | 4.91 | 5.79 | 3.95 | 9.25 | 5.13 | 2.44 | 4.58 | 6.34 | 6.39 | 4.34 | 4.08 | 5.9 | 3 | 2.02 | 2.96 | 1.84 | 1.34 | 3.78 | 4.16 | 3.21 | 3.8 | 3.6 | 4.2 | 4.3 | 3.69 | 4.04 | 3.07 | 2.67 | 3.1 | 3.2 | 3.1

## Slide 13: Extraction Tests
Evaluates metals and metalloids that are rinsed from the sample when it is exposed to water
Bottle roll or column rinse tests
Generally use deionized water or simulated precipitation as an extraction fluid
Examples
  Synthetic Precipitation Leach Procedure (EPA Method 1312)
  Meteoric Water Mobility Procedure (ASTM Method E2242-07)
  USGS Field Leach Test
Modified SPLP extraction tests used at Formosa
  Reduced water to rock ratio as compared with standard SPLP
Improving Remediation Planning though Effective Mine Material Delineation, Formosa Mine Superfund Site

## Slide 14: Modified SPLP vs. Paste pH- Cu
Improving Remediation Planning though Effective Mine Material Delineation, Formosa Mine Superfund Site

## Slide 15: Development of Field Paste pH Criterion- Cu
Improving Remediation Planning though Effective Mine Material Delineation, Formosa Mine Superfund Site
MWMP Screening Criteria based on Site Conceptual Model

## Slide 16: Development of Field Paste pH Criterion- Cd
Improving Remediation Planning though Effective Mine Material Delineation, Formosa Mine Superfund Site

## Slide 17: Development of Field Paste pH Criterion- Zn
Improving Remediation Planning though Effective Mine Material Delineation, Formosa Mine Superfund Site

## Slide 18: Analysis of Field Paste pH Criterion
Improving Remediation Planning though Effective Mine Material Delineation, Formosa Mine Superfund Site
 | Paste pH |  | Paste pH+ Lithology | 
Analyte | False Negative (%) | False Positive (%) | False Negative (%) | False Positive (%)
Cadmium | 5 | 11 | 2 | 10
Copper | 7 | 2 | 4 | 0
Zinc | 8 | 2 | 3 | 1
Decision Error Rates
Field Paste pH Criterion: 4.6 su
Weight of Evidence Approach Improves Decision Error Rate

## Slide 19: GIS Analysis based on Field Paste pH Criterion
Improving Remediation Planning though Effective Mine Material Delineation, Formosa Mine Superfund Site

## Slide 20: Use of Field Portable XRF
Useful to measure total metals concentrations
Total metals concentrations do not necessarily correlate to potential water quality effects
Used at Formosa to evaluate boundary between mine materials and natural soils
Samples prepared in the field using disposable -1.5 mm sieves
XRF data validated with laboratory check samples
Improving Remediation Planning though Effective Mine Material Delineation, Formosa Mine Superfund Site

## Slide 21: FPXRF Accuracy- Zn
Improving Remediation Planning though Effective Mine Material Delineation, Formosa Mine Superfund Site
Chart: Lab Zinc Concentration (mg/kg)
| 301 | 315 | 163 | 227 | 1360 | 3390 | 992 | 371 | 844 | 918 | 250 | 247 | 369 | 63.7 | 512 | 112 | 260 | 1380 | 100 | 898 | 76.8 | 171 | 441 | 85.6 | 246 | 376 | 179 | 142 | 472 | 993 | 246 | 181 | 213 | 410 | 381 | 779 | 303 | 471 | 700 | 380 | 320 | 191 | 176 | 210 | 1420 | 434 | 933 | 756 | 261 | 581 | 122
Zn | 0.0079198 | -0.27417 | -0.071105 | -0.15737 | -0.74636 | 0.44762 | -0.14652 | -0.10141 | 0.016579 | -0.26199 | -0.1829 | -0.18847 | 0.00058746 | -0.054808 | 0.24275 | -0.053285 | -0.10479 | -0.59231 | 0.005657 | -0.1324 | 0.030048 | -0.051392 | -0.2706 | -0.0080069 | -0.037054 | -0.26562 | 0.075935 | 0.11851 | -0.030526 | -0.21107 | 0.016536 | -0.14332 | -0.0030679 | -0.33431 | -0.23209 | -0.64682 | -0.23216 | 0.30211 | -0.3171 | -0.29336 | -0.30783 | -0.15729 | -0.072388 | -0.17811 | -13.768 | -1.327 | -0.3906 | -0.99851 | -0.68237 | -0.25465 | -0.54251 | -0.14441
zero line | 0 | 0
FPXRF data biased low at concentrations over approximately 200 mg/kg

## Slide 22: Formosa FPXRF Data- Zn
Improving Remediation Planning though Effective Mine Material Delineation, Formosa Mine Superfund Site
Data are positively skewed
Log transformation suggests bimodal distribution
Hypothesized to be related to sampling of the geological boundary between mine materials and natural soils

## Slide 23: Formosa FPXRF Data
Improving Remediation Planning though Effective Mine Material Delineation, Formosa Mine Superfund Site

## Slide 24: FPXRF Inspection Criteria
Improving Remediation Planning though Effective Mine Material Delineation, Formosa Mine Superfund Site
Inspection criteria for Cu and Zn based on breakpoint of cumulative probability plot

## Slide 25: Application of FPXRF Inspection Criteria
Improving Remediation Planning though Effective Mine Material Delineation, Formosa Mine Superfund Site

## Slide 26: Adding the Third Dimension
Improving Remediation Planning though Effective Mine Material Delineation, Formosa Mine Superfund Site
  Depth shown as thickness isopachs
3-dimensional model generated in ArcGIS Spatial Analyst to support volume estimation
Depth and volume characterized in sufficient detail to support feasibility study analyses

## Slide 27
Improving Remediation Planning though Effective Mine Material Delineation, Formosa Mine Superfund Site
Study Questions
  ARD potential?
  Metals leaching potential?
Horizontal and vertical extent?
  Volume?
Study Conclusions
  ARD generating mine materials identified
  Mine materials that leach metals delineated
    Evaluated with respect to CSM
    Known and acceptable decision error rates
Areal extent, depth and volume defined
What Did We Learn?

## Slide 28: Conclusions
Improving Remediation Planning though Effective Mine Material Delineation, Formosa Mine Superfund Site
Rapid field geochemical characterization performs well at answering study questions
Method applicable at various project phases and in various levels of detail
Provides for efficient and detailed characterization, while managing investigation costs
  Thanks to our partners!
  US EPA
  US Bureau of Land Management
  Oregon DEQ
  USGS